(Supplementary Materials)

Pyrolysis Kinetics of Coking Coal Mixed with Biomass under Non-Isothermal and Isothermal Conditions

Ha Myung Jeong1, Myung Won Seo2, Sang Mun Jeong1*, Byung Ki Na1,

Sang Jun Yoon2, Jae Goo Lee2, and Woon Jae Lee3

1 Department of Chemical Engineering, Chungbuk National University, 52 Naesudong-ro, Heungdeok-gu, Cheong ju 361-763, Republic of Korea

2 Clean Fuel Laboratory, Korea Institute of Energy Research (KIER), 152 Gajeong-ro, Yuseong-gu, Daejeon 305-343, Republic of Korea

3 POSCO Technology Center, POSCO, 6261 Donghaean-ro, Nam-gu, Po hang 790-300, Republic of Korea

*  Corresponding author.

Tel.: 82-43-269-3369, Fax: 82-43-269-2370, E-mail: smjeong@chungbuk.ac.kr (Sang Mun Jeong)

Fig. S1. (a) TG and (b) DTG curves of the WC/B samples and (c) TG and (d) DTG curves of the HC/B samples under non-isothermal conditions.

Fig. S2. Effects of biomass blend ratio on (a) TG curves and (b) reactivity of WC/B samples at 700°C and effects of final temperature on (c) TG curves and (d) reactivity of 15B85WC sample under isothermal conditions.

Fig. S3. Effects of biomass blend ratio on (a) TG curves and (b) reactivity of HC/B samples at 700°C and effects of final temperature on (c) TG curves and (d) reactivity of 15B85HC samples under isothermal conditions.

Fig. S4. SEM images of (a) 85B15WC char sample at 700°C under non-isothermal conditions (×100) and (b) its magnification (×1000) and (c) 85B15HC char sample at 700°C under non-isothermal conditions (×100) and (d) its magnification (×1000).

Table S1. The proximate and ultimate analyses and the calorific value of samples

| Samples | WC (Weak-Coking) Coal | HC (Hard-Coking) Coal | Yellow poplar (B) |
| --- | --- | --- | --- |
| Proximate analysis (wt%, adb) |  |  |  |
| Moisture | 2.21 | 1.31 | 5.75 |
| Volatile matter | 35.35 | 33.04 | 77.12 |
| Fixed Carbon | 53.76 | 57.98 | 16.25 |
| Ash | 8.68 | 7.67 | 0.88 |
| Ultimate analysis (wt%, db) |  |  |  |
| C | 81.94 | 86.97 | 48.64 |
| H | 6.04 | 5.78 | 5.83 |
| O* | 2.11 | 1.63 | 45.1 |
| N | 9.38 | 4.69 | 0.43 |
| S | 0.53 | 0.93 | 0 |
| Calorific value (kcal/kg) | 7,209 | 7,784 | 4,701 |

* Calculated by difference.

Table S2. Kinetic parameters of the WC/B and HC/B blends under non-isothermal conditions

| Samples | Conversion [%] |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 20 | 30 | 40 | 50 | 60 | 70 | 80 |
| 0B100WC | Ea(kJ/mol) | 252.08 | 274.61 | 288.99 | 307.78 | 392.67 | 579.40 | 482.30 |
|  | A | 4.59 × 1015 | 1.27 × 1017 | 8.22 × 1017 | 9.18 × 1018 | 2.19 × 1024 | 6.19 × 1035 | 2.29 × 1027 |
| 10B90WC | Ea(kJ/mol) | 247.42 | 233.71 | 267.79 | 365.65 | 289.58 | 456.44 | 374.30 |
|  | A | 1.26 × 1019 | 1.22 × 1017 | 3.07 × 1019 | 8.72 × 1026 | 2.51 × 1018 | 3.06 × 1029 | 1.82 × 1023 |
| 15B85WC | Ea(kJ/mol) | 249.75 | 228.72 | 309.20 | 251.42 | 331.23 | 269.46 | 229.13 |
|  | A | 1.69 × 1018 | 6.1 × 1015 | 7.84 × 1020 | 5.61 × 1015 | 1.47 × 1021 | 2.21 × 1016 | 6.74 × 1012 |
| 20B80WC | Ea(kJ/mol) | 127.70 | 147.91 | 176.92 | 149.57 | 273.28 | 377.87 | 422.18 |
|  | A | 1.53 × 108 | 3.33 × 109 | 4.87 × 1011 | 1.98 × 108 | 1.31 × 1017 | 1.41 × 1024 | 1.69 × 1026 |
| 30B70WC | Ea(kJ/mol) | 162.21 | 205.94 | 270.21 | 239.19 | 254.99 | 372.72 | 336.63 |
|  | A | 3.99 × 1011 | 7.93 × 1014 | 8.69 × 1019 | 1.15 × 1017 | 5.49 × 1017 | 5.17 × 1024 | 1.62 × 1021 |
| 0B100HC | Ea(kJ/mol) | 221.48 | 163.70 | 195.88 | 211.59 | 175.67 | 244.68 | 272.45 |
|  | A | 1.95 × 1013 | 1.08 × 109 | 1.86 × 1011 | 1.75 × 1012 | 3.33 × 109 | 6.69 × 1013 | 2.10 × 1014 |
| 10B90HC | Ea(kJ/mol) | 237.95 | 346.86 | 238.61 | 277.60 | 276.61 | 363.65 | 400.98 |
|  | A | 4.19 × 1016 | 2.3 × 1024 | 5.44 × 1014 | 2.41 × 1017 | 1.03 × 1017 | 3.85 × 1022 | 8.33 × 1023 |
| 15B85HC | Ea(kJ/mol) | 149.74 | 162.95 | 146.16 | 229.55 | 281.01 | 291.41 | 385.60 |
|  | A | 8 × 109 | 4.02 × 1010 | 6.96 × 108 | 1.19 × 1014 | 3.79 × 1017 | 8.42 × 1017 | 4.06 × 1023 |
| 20B80HC | Ea(kJ/mol) | 209.01 | 203.11 | 211.59 | 267.30 | 246.76 | 287.33 | 359.91 |
|  | A | 2.99 × 1015 | 1.99 × 1014 | 5.55 × 1014 | 3.84 × 1018 | 2.36 × 1015 | 8.25 × 1017 | 2.19 × 1022 |
| 30B70HC | Ea(kJ/mol) | 120.72 | 113.40 | 140.34 | 117.73 | 88.71 | 209.35 | 164.70 |
|  | A | 6.79 × 107 | 7.32 × 106 | 9.88 × 108 | 1.01 × 107 | 5.40 × 103 | 2.73 × 1012 | 6.95 × 108 |

Table S3. BET analysis of the WC/B and HC/B blend chars (non: non-isothermal condition, iso: isothermal condition) with variation of pyrolysis temperature

|  | 15B85WC char |  |  |  | 15B85HC char |
| --- | --- | --- | --- | --- | --- |
|  | 500°C | 600°C | 700°C | 800°C |  |
| Surface area (m2/g) | 0.22(non) 7.3(iso) | 19.11(non) 63.49(iso) | 41.62(non) 66.16(iso) | 6.89(non) 37.6(iso) | n.d.* |
| Average pore size (Å) | 17.4(iso) | 9.3(iso) | 1.9(non) 2.8(iso) |  | n.d.* |

*not detectable